Supporting Information

Neodymium coordination polymers with propionate, succinate and mixed succinate-oxalate ligands: synthesis, structures and spectroscopic characterization

Nicholas Scales a, Yingjie Zhang a,*, Mohan Bhadbhade b, Inna Karatchevtseva a, Linggen Kong a, Gregory R. Lumpkin a, Feng Li c

Fig. S1. PXRD patterns of 1 (left) and 3 (right) with the measured on top of the simulated ones.

Fig. S2. Thermogravimetric and differential thermal analysis result of 1 (left) and 3 (right).

Table S1. Raman bands and assignments for 1, 2 and 3.

| Raman band position (cm-1) | Band assignment |
| --- | --- |
| Complex 1 |  |
| 1621 w, sh | Lattice water, (HOH) deformation vibration |
| 1555 m, br | as (COO) |
| 1451 s, a shoulder | as (CH3) + (CH2) deformation vibrations (higher frequency shoulder) |
| 1422 s | s (COO) |
| 1377 m | s (CH3) |
| 1301 m | (CH2) wagging vibrations |
| 1250 m | (CH2) twisting vibrations |
| 1077 s, 1029 s + 1009 sh, 899 vs | Skeletal (CCC) + (CC) stretching vibrations |
| 815 w | (OCO) in-plane bending vibrations |
| 740 w | (CH2) rocking vibrations |
| 679 m | (OCO) out-of-plane bending vibrations |
| 643 w, br | Vibrational modes of coordinated water molecules |
| 513 w, br | (CC) deformation vibrations |
| 311 w | (MO) |
| < 300 | (COM) + (CH3) (torsional vib) + lattice modes |
| Complex 2 |  |
| 1620 vw, sh | Lattice water, (HOH) deformation vibration |
| 1589 w, 1534 and 1515 m-w, br | as (COO) |
| 1461 s and 1440 sh | (CH2) deformation vibrations |
| 1409 and 1401 split peak, m | s (COO) |
| 1327-1287 w | (CH2) wagging vibrations |
| 1216, 1167 m | (CH2) twisting vibrations |
| 1055 m, 1016, 1004, 982 m-s, 910, 901, 879 vs | Skeletal (CC) stretching vibrations, chain vibration, including CCC and CCCC |
| 815 w | (OCO) in-plane bending vibrations |
| 760 and 741 w | (CH2) rocking vibrations |
| 660 vw | Vibrational modes of coordinated water molecules |
| 629 m | (OCO) out-of-plane bending vibrations |
| 580 w | (OCO) rocking |
| 522456, vw | (CC) deformation modes |
| 324 w | (MO) |
| < 300 | (COM) + lattice modes |
| Complex 3 |  |
| 1620 vw, sh | Lattice water, (HOH) deformation vibration |
| 1608 w, 1570 and 1525 m-w, br | as (COO) |
| 1462 s | (CH2) deformation vibrations and (CO) specific for oxalate ligand |
| 1414 m | s (COO) |
| 1326 - 1278 m-w | (CH2) wagging vibrations |
| 1222, 1178 m-w | (CH2) twisting vibrations |
| 1051 m, 1005, 971, 942 m, 902, 880 vs | Skeletal (CC) stretching vibrations, chain vibration, including CCC and CCCC |
| 819 m | (OCO) in-plane bending vibrations |
| 738 and 703 w | (CH2) rocking vibrations |
| 642 m | (OCO) out-of-plane bending vibrations |
| 667 vw | Vibrational modes of coordinated water molecules |
| 578 w | (OCO) rocking |
| 519-456, w-m | (CC) deformation modes |
| 327 w | (MO) |
| < 300 | (COM) + lattice modes |