Effect of Ti-metal addition on hot-isostatically pressed (HIPed) Synroc-C

Rifat Farzana1, Pranesh Dayal1, Anton Peristyy1, Phillip Sutton1, Zaynab Aly1, Robert D. Aughterson1, Thanh Ha Nguyen1, Michelle Yeoh1,2, Pramod Koshy2, Daniel J. Gregg1,*

1 Australian Nuclear Science and Technology Organisation, Locked Bag 2001, Kirrawee DC, New South Wales, Australia

2 School of Materials Science and Engineering, UNSW Sydney, NSW 2052, Australia

* Corresponding author. Tel.: +61 2 9717 7075; fax: +61 2 9717 9225.

E-mail address: dgg@ansto.gov.au

Table S1: Theoretical redox environment of Synroc C phases over varying Ti metal addition.

|  | Effective oxidation state |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Ti addition, % w/w | Before Calcination | After Calcination | 0% | 2% | 4% | 8% |
| Ru | 4 | 0 | 0 | 0 |  |  |
| Pd | 2 | 0 | 0 | 0 |  |  |
| Ni | 2 | 0 | 0 | 0 |  |  |
| Ag | 1 | 0 | 0 | 0 |  |  |
| Cs | 1 | 1 | 1 | 1 |  |  |
| Ca | 2 | 2 | 2 | 2 |  |  |
| Ba | 2 | 2 | 2 | 2 |  |  |
| Sr | 2 | 2 | 2 | 2 |  |  |
| Al | 3 | 3 | 3 | 3 |  |  |
| Nd | 3 | 3 | 3 | 3 |  |  |
| Gd | 3 | 3 | 3 | 3 |  |  |
| Y | 3 | 3 | 3 | 3 |  |  |
| Zr | 4 | 4 | 4 | 4 |  |  |
| Cr | 3 | 3 | 3 | 2 or 0 | 0 |  |
| Mo | 6 | 4 | 4 | 0 |  |  |
| Fe | 3 | 2 | 2 | 0 |  |  |
| Ce | 4 | 4 | 4 | 3 |  |  |
| Ti | 4 | 4 | 4 | 3.937 (Ti12O23+20TiO2) | 3.72 (Ti7O13) | 3.333 (Ti3O5) |
| Redox condition, pfO2 |  |  | ~10-11 | 10-13 | 10-14 | >10-16 |

Table S2: Phase compositions of the newly formed non-Synroc phases formed in the 8 wt.%Ti metal sample as determined from TEM-EDS analyses.

| Name | Phase composition1 |
| --- | --- |
| Manetoplumbite (AB12O19)2 | Ca(Al2.2Ti7.5Fe0.04Y0.04Zr1.67)O19 |
|  | (Ba0.95Ca0.1)(Al0.3Ti10.3Fe0.05Zr0.5Mo0.23)O19 |
| Loveringite (AB21O38)3 | (Ca0.8Sr0.07Nd0.1)(Al0.9Ti18.6Fe0.06Zr1Ag0.1Mo0.5)O38 |
| Cs,Mo-rich phase (at.%) | Cs: ~3-5, Mo: ~2-5, Al: ~1-2, Ca: ~1-11, Ti: ~15-20 with minor Fe, Zr, Ce, Nd and Gd. |

1 Oxygen content was not measured, 2 assuming a total of 1 cations on the A-sites, 3 assuming a total 1 cations on the A-sites.

Fig. S1: Goodness of fit for quantitative analysis in the 0 wt.% Ti sample.

Fig. S2: High magnification SEM image showing the Cs and Mo rich compounds in the 0 wt.% Ti sample.

The following sample list is added for internal use only: the sample IDs are linked to the internal numbering system to simplify the sample identification for future.

Sample identification:

- L200044 (0 wt.% Ti)

- L200067 (2 wt.% Ti)

- L200068 (4 wt.% Ti)

- L200069 (8 wt.% Ti)