Supporting Information

A Software for Evaluating Ionic Conductivity of Inorganic–Polymer Composites Solid Electrolytes

Yuqing Ding1, Bing He2, Da Wang1, Maxim Avdeev3,4, Yajie Li1, Siqi Shi1,5*

1School of Materials Science and Engineering, Shanghai University, Shanghai 200444, China

2School of Computer Engineering and Science, Shanghai University, Shanghai 200444, China

3Australian Nuclear Science and Technology Organisation, Sydney 2232, Australia

4School of Chemistry, The University of Sydney, Sydney 2006, Australia

5Materials Genome Institute, Shanghai University, Shanghai 200444, China

*E-mail: sqshi@shu.edu.cn (Siqi Shi)

Table S1 Performance comparison among various solid electrolytes

| Solid electrolytes |  | σ (S cm−1) (RT) | TLi+ (RT) | ECW (V) | Flexibility | Thermal stability | Interfacial property |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Polymer |  | 10−7~10−5 | 0.2~0.5 | ~4 | Excellent | Inferior | Excellent |
| Inorganic | Oxide | 10−4~10−3 | 1 | >5 | Inferior | Excellent | Inferior |
|  | Sulfide | 10−3~10−2 | 1 | 2~3 | Medium | Good | Good |
| IPCSEs |  | 10−4~10−3 | >0.5 | >5 | Excellent | Medium | Good |

σ: ionic conductivity;TLi+: ionic transference numbers; RT: room-temperature; ECW: electrochemical window

Table S2 Conductivity of the three phases of IPCSEs (S cm−1, RT)

| IPCSEs | Polymer matrix (σA) | Inorganic filled phase (σB) | Amorphous polymer (σC) |
| --- | --- | --- | --- |
| PAN/LiClO4-LLTO[1,2] | 3.62×10−7 | 1.0×10−3 | 1.26×10−2 |
| PEO/LiClO4-LLZNO[3,4,5] | 2×10−8 | 8×10−4 | 1.5×10−4 |
| PEO/LiTFSI-LLTO[6,7] | 2.2×10−6 | 1.0×10−3 | 5.31×10−3 |
| PEO(Li-salt-free)-LLZTO[8,9] | 2.3×10−6 | 1.6×10−3 | 1.5×10−5 |
| PEO/LiCF3SO3-Al2O3[10] | 2×10−8 | insulation | 1.1×10−5 |
| PEO/LiClO4-SiO2[11,12] | 8.1×10−8 | insulation | 5.5×10−5 |

In the simulation, τA，τB and τC represent the time step required for walkers to successfully pass A, B and C bonds, respectively. τA-1，τB-1 and τC-1represent the migration rate of walkers through different bonds, which is proportional to the conductivity of different phases, σA，σB and σC. In this work, these three values are given by the three-phase conductivity σA，σB and σC. We assume that τ=1/σ.

Table S3 EMT models for effective conductivity of a composite material

| Maxwell-Wagner Theory | σe-σBσe+(d-1)σB=(1-ga)σA-σBσA+(d-1)σB |
| --- | --- |
| Asymmetric BEM | (σA-σe)dσe-1 =gad(σA-σB)dσB-1 |
| Symmetric BEMT | gaσB-σeσB+(d-1)σe+1-gaσA-σeσA+d-1σe=0 |
| McLachlan Generalized EMT | ga(σB)1/t-(σe)1/t(σB)1/t+[ge-1-1](σe)1/t+1-ga(σA)1/t-σe1/t(σA)1/t+ge-1-1σe1/t=0 |
| Series Brick-Layer Model | σe-1=gaσB-1+(1-ga)σA-1 |
| Parallel Brick-Layer Model | σe=gaσB+(1-ga)σA |
| Landau-Lifshitz | σe1/3=gaσB1/3+(1-ga)σA1/3 |
| Hamilton-Crosser | σe-σAσe+(n-1)σA=gaσB-σAσB+(n-1)σA |

σe: effective composite conductivity; ga: reinforcement volume fraction; ge: effective percolation threshold; t: effective percolation slope; d: system dimensionality; n: inclusion shape factor; BEMT: Bruggeman Effective Medium Theory

Figure S1 Four shapes of inorganic filler RRM schematic diagram: (a) nano-particles; (b) nano-wires; (c) nano-sheets; (d) nano-networks

Figure S2 Inorganic filler ordered arrangement diagrams, three shapes of inorganic fillers are (a) aligned one-dimensional nano-wires; (b) aligned two-dimensional nano-sheets; (c) aligned three-dimensional nano-networks

Reference:

1. Liu, W.; Lee, S. W.; Lin, D.; Shi, F.; Wang, S.; Sendek, A. D.; Cui, Y. Enhancing ionic conductivity in composite polymer electrolytes with well-aligned ceramic nanowires. Nat. Energy 2017, 2, 1-7.

2. Liu, W.; Liu, N.; Sun, J.; Hsu, P. C.; Li, Y.; Lee, H. W.; Cui, Y. Ionic conductivity enhancement of polymer electrolytes with ceramic nanowire fillers. Nano Lett. 2015, 15, 2740-2745.

3. Song, S.; Wu, Y.; Tang, W.; Deng, F.; Yao, J.; Liu, Z.; Hu, R.; Alamusi; Wen, Z.; Lu, L. Composite solid polymer electrolyte with garnet nanosheets in poly (ethylene oxide). ACS. Sustainable Chem. Eng. 2019, 7, 7163-7170.

4. Wen, Z. Y.; Wu, M.; Itoh, T.; Kubo, M.; Lin, Z. X.; Yamamoto, O. Effects of alumina whisker in (PEO)8-LiClO4-based composite polymer electrolytes. Solid State Ionics 2002, 148, 185-191.

5. Ohta, S.; Kobayashi, T.; Asaoka, T. High lithium ionic conductivity in the garnet-type oxide Li7-XLa3(Zr2-X, NbX)O12 (X=0–2). J. Power Sources 2011, 22, 3342-3345.

6. Fan, L. Z.; He, H.; Nan, C. W. Tailoring inorganic–polymer composites for the mass production of solid-state batteries. Nat. Rev. Mater. 2021, 6, 1003-1019.

7. Bae, J.; Li, Y. T.; Zhang, J.; Zhou, X. Y. A 3D Nanostructured Hydrogel-Framework-Derived High-Performance Composite Polymer Lithium-Ion Electrolyte. Angew. Chem. Int. Ed. 2018, 57, 2096-2100.

8. Zaman, W.; Hortance, N.; Dixit, M. B.; De Andrade, V.; Hatzell, K. B. Visualizing percolation and ion transport in hybrid solid electrolytes for Li–metal batteries. J. Mater. Chem. A 2019, 7, 23914-23921.

9. Zhang, J.; Zhao, N.; Zhang, M.; Li, Y.; Chu, P. K.; Guo, X.; Di, Z.; Wang, X.; Li, H. Flexible and ion-conducting membrane electrolytes for solid-state lithium batteries: Dispersion of garnet nanoparticles in insulating polyethylene oxide. Nano Energy 2016, 28, 447-454.

10. Li, Y.; Zhao, Y.; Cui, Y.; Zou, Z.; Wang, D.; Shi, S. Screening polyethylene oxide-based composite polymer electrolytes via combining effective medium theory and Halpin-Tsai model. Comput. Mater. Sci. 2018, 144, 338-344.

11. Yu, X.; Bates, J.; Jellison, G.; Hart, F. A stable thin‐film lithium electrolyte: lithium phosphorus oxynitride. J. Electrochem. Soc. 1997, 144, 524.

12. Wieczorek, W.; Such, K.; Florjanczyk, Z.; Stevens, J. Polyether, polyacrylamide, LiClO4 composite electrolytes with enhanced conductivity. J. Phys. Chem. 1994, 98, 6840-6850.