Radium and strontium binding by a modified bauxite refinery residue – Isotope exchange studies of pH-dependence, reversibility and aging

M.W. Clark1,2*, J.J. Harrison3, T.E. Payne1,3, M.J. Comarmond3, S. Thiruvoth3, H. Wong3, and L. Mokhber Shahin3

1 School of Environment, Science and Engineering, Southern Cross University, PO Box 157, Lismore, NSW 2480, Australia

2 Southern Cross Geoscience, Southern Cross University, PO Box 157, Lismore, NSW 2480, Australia

3 Australian Nuclear Science and Technology Organisation, Locked Bag 2001 Kirrawee DC NSW 2232. Australia

* Corresponding Author: malcolm.clark@scu.edu.au

# Abstract

The pH-dependence and reversibility of radium (Ra) and strontium (Sr) binding onto a modified bauxite refinery residue (MBRR), and the effects of sample aging, were studied in laboratory uptake / leaching experiments.  Natural 226Ra and stable strontium (Srnat) were contacted with MBRR in an 8-day loading period (equilibrium pH ≈ 8.5).  Following the addition of exchange isotopes 228Ra and 85Sr, the samples were then leached in pH-dependent experiments, where the pH was decreased incrementally from 9 to 3 over seven hours.  A further suite of samples was aged at 4°, 23°, and 65°C for 6-months after the initial addition of 226Ra and Srnat and then studied in a similar set of pH-dependent exchange experiments.  Relative concentrations of the Ra and Sr isotope pairs (226Ra/228Ra and Srnat/85Sr) provided insights into the adsorption strength, incorporation, reversibility and aging effects.  The Srnat data showed that the release of bound Sr from aged MBRR samples as the pH decreases is substantially less than the unaged sample, showing that during the aging period, Sr has been incorporated in less accessible phases.  It appears that the uptake of 228Ra by the higher temperature aged samples is somewhat stronger than the unaged samples, however Ra isotope exchange plots for aged and unaged samples are similar.  Consequently, the stronger binding of 228Ra by the higher temperature aged samples is probably driven by translocation to kinetically less favourable surface sites rather than a significant incorporation of radium within the mineral solids during aging.

Keywords: iron oxides; trace-metal redistributions; improved binding; surface bindings; modified bauxite refinery residues

# Introduction

Radium is an alkaline earth element found in trace amounts in all uranium-bearing rocks and ores, hence almost all Ra in drinking water supplies occurs naturally (Milvy and Cothern, 1990; Rachkova et al., 2010), although anthropogenic activities (e.g. mining, phosphate production, and agriculture) can lead to significant Ra inputs (Baeza et al., 2006; Yoshida and Yoshikawa, 2009).  The concentrations of natural Ra isotopes in water reflect the origin of the water, the geology and geochemistry of the host formation, including factors such as soil type and pH (Baeza et al., 1995; Rachkova et al., 2010; Thiry and Van Hees, 2008).  Moreover, the chemical forms in which Ra is present in the soil and the concentration also determine how readily Ra becomes released to the groundwater (Chau and Kopeć, 2010; Vaaramaa et al., 2003).

Strontium is also naturally abundant with no known natural radio-isotopes and is typically found as the minerals celestite (SrSO4), and strontianite (SrCO3).  Natural strontium is comprised of various stable isotopes including 88Sr, 86Sr, 87Sr and 84Sr (in decreasing order of abundance) and is referred to in this paper as Srnat.  However, some strontium isotopes (particularly 90Sr) are fission products arising from nuclear activities.  Until the atmospheric testing ban, nuclear explosions caused significant quantities of radio-strontium to be released to the environment (Chiang et al., 2010; Steinhauser et al., 2015; Tracy and Prantl, 1983).  90Sr is also present in nuclear waste and can be released to the environment in low levels during the operation of nuclear facilities or as a consequence of major nuclear accidents.

Given that Ra and Sr are chemically very similar to Ca (Rihs et al., 2000; Schmidt and Cochran, 2010; Van Beek et al., 2004), inhalation, ingestion or body exposure to Ra or radioactive Sr have the potential to cause harm to human health, through the replacement of Ca in tissues.  Accordingly, Ra has been implicated as a major cause of bone cancer and other disorders (Mays, 1988; Mays et al., 1985; Raabe et al., 1983).  Consequently, Ra-rich water usually undergoes chemical treatment before being considered suitable for human consumption.  In the United States of America, several areas of the country have higher rates of disorders, linked to elevated Ra concentrations (Clark et al., 2011; Shao et al., 2009; Sturchio et al., 2001; Vaaramaa et al., 2003).  For example, many areas of Missouri have groundwater Ra concentrations which exceed the U.S. EPA guidelines for safe human consumption of 0.185 Bq.L-1 (5 pCi L-1; (USEPA, 1976, 1996).  Clark et al. (2011) have shown that modified bauxite refinery residues (MBRR) may be used to remove Ra from ground waters, and their data suggests that Sr could be removed by a similar mechanism.

MBRR materials are chemically and physically modified products derived from Bayer process alumina refining residues, where pH is reduced from about 13 to about 8.5, and soluble alkalinity is converted to solid alkalinity.  Consequently, MBRR contains a complex mix of minerals including the following: abundant hematite, boehmite, gibbsite, sodalite, quartz, cancrinite and whewellite; minor aragonite, brucite, calcite, diaspore, ferrihydrite, anhydrite/gypsum, hydrocalumite, hydrotalcite, and p-aluminohydrocalcite; and a few low-solubility trace minerals (Clark et al., 2011).  The exact composition and geochemical characteristics of a MBRR depend on the origin of the bauxite, the operational procedures used in the alumina refinery, and the concentration and balance of calcium and magnesium used to modify the residue (McConchie et al., 2001).  MBRR can be modified further chemically and/or physically by means such as acid treatments, blending with additional mineral components, and pelletisation, leading to a range of modified materials marketed under the trade name Bauxsol™.  MBRR is extremely fine grained, typically 90% is <10 µm in diameter, and it has a very high surface/volume ratio (up to over 100 m2 g-1).  Additionally, it has high metal binding capacities, moderate acid-neutralizing capacity, is largely insoluble, and is highly non-dispersive (Genç-Fuhrman, 2004; Lapointe et al., 2006; McConchie et al., 1999).

The acid-neutralising capacity (ANC) of MBRR ranges from 4 - 7 moles H+ kg-1 at pH 7 to about 14 moles H+ kg-1 at pH 5.  The ANC is mainly provided by low-solubility carbonate, hydroxide and hydroxyl-carbonate minerals formed during the modification step.  In addition, many of the minerals providing the ANC react slowly and, at low pH, surface adsorption onto variably charged iron- and aluminium oxyhydroxides also increases the effective ANC (McConchie et al., 1999).  The residual ANC of pellet material is 6-7 moles H+ kg-1 at pH 5.5.  Similarly, the ability of the minerals to bind trace metals (>1500 meq.kg-1), phosphate, and other oxy-anions is also strongly dependent on time and pH.  Although initial metal binding seems complete within 24 hours, metal binding will often continue, although more slowly, for many months.  Furthermore, recent work indicates that the longer the material is left to age before metal extraction, the more tightly metals are bound (Clark et al., 2009).

In this study the uptake and reversibility of Ra and Sr adsorption to MBRR are investigated to determine:

(i) the optimal pH and partitioning of Ra and Sr between the solid and liquid phases;

(ii) the reversibility of the Ra and Sr binding;

(iii) the effects that sample aging has on the reversibility of binding; and

(iv) the effects that pre-existing Ra and Sr pools may have on isotopic exchange.

Radionuclide exchange techniques were applied in this study, because they enable the capability to simultaneously study different isotopes in a single experiment, have a direct applicability to the behaviour of radionuclides present in radioactive waste or fallout, and allow the study of the mechanisms, reversibility and kinetics of environmental reactions under controlled conditions (Payne et al., 2004).  These techniques can be used to study both short-term reversible adsorption between liquid and solid phases as well as the longer-term incorporation of radionuclides during sample aging and transformation processes and their subsequent leaching properties. As such, they are particularly suitable for these laboratory studies of environmental processes involving Ra and Sr.

2.	Materials and Methods

# 2.1	Modified bauxite refinery residue

A modified bauxite refinery residue was obtained from Virotec Global solutions Pty Ltd under the trade name Bauxsol™; this Bauxsol™ (MBRR) was prepared from Euralumina BRR (Sardinia).  MBRR is generally reported as having a pH ≈8.5 through the precipitation of hydroxyl-carbonates, however, these precipitates can revert to simple hydroxides and carbonates.  The MBRR sample supplied for this work had a reaction pH of 10.2, indicating some reversion had occurred (Palmer and Frost, 2010; Palmer et al., 2010).  However, this higher pH was found to be poorly buffered, suggesting that only a minor amount of reversion had occurred.

The MBRR contains Srnat and Ra isotopes (226Ra and 228Ra), which must be considered in the interpretation of the experimental data.  The percentage (by mass) of 226Ra, 228Ra and Srnat pre-existing in the MBRR used in these experiments are 4x10-10 %, 2x10-12 % and 0.08%, respectively.  Consequently, the pre-existing Ra concentrations, which are likely to exist predominantly as inaccessible forms contained within very-stable heavy minerals, are insignificant compared to the experimental loading concentrations.  However, the Sr concentrations are sufficiently high that they need to be considered in interpreting the experimental results, as later discussed.

# 2.2	Preparation of initial equilibration solutions and isotopic exchange solutions

Solutions of Srnat were prepared using a 1000 ppm High Purity Standards Sr(NO3)2 solution (lot #608936 Catalogue Number 100053-1).  Strontium-85 exchange isotope solutions were prepared using an Eckert & Ziegler nominal liquid 85Sr solution (source code: 1331-18-2).  Strontium-85 was used in this study as it is conveniently detected by its gamma emission.  226Ra solutions and 228Ra exchange solutions were prepared using ANSTO internal stock solutions which have been independently verified (Zawadzki et al., 2017).

# 2.3	Initial pre-equilibration of MBRR with radium and strontium

The first part of the experiment was the initial loading of MBRR with associated Srnat and 226Ra.  The predominant process leading to binding is surface adsorption, but if diffusion is occurring, some migration from surface sites to deeper layers would also occur.  In these experiments, stock solutions containing Srnat and 226Ra were equilibrated over an 8-day (192 hrs) period with MBRR.  It has been previously shown that over this time, adsorption of trace metals reaches a steady state (Clark et al., 2009; Collins et al., 2014).  The solid to liquid ratio for this initial part of the experiment was 1 g of MBRR per 40 mL of liquid.  Four loading solutions were prepared containing nominal Srnat concentrations of 1.14 x 10-5 M and 2.34 x 10-5 M, or 226Ra concentrations of 5 x 10-11 M and 1 x 10-10 M, respectively.  For each metal concentration, two 1.25 g samples of MBRR were accurately weighed into 50 mL centrifuge tubes prior to addition of the relevant loading solution, sealed and equilibrated in a thermostatted shaking water-bath set at 23°C.  Samples were periodically removed from the water-bath (≈ twice daily) and vigorously shaken to completely re-suspend heavier mineral particles.  Due to the strong buffering capacity of the MBRR, the pH of these solutions stabilised at approximately 8.5.  Following equilibration, samples were twice centrifuged at 4500 rpm for 10 minutes to separate solids and liquid, and the supernatant liquor collected for analysis.  The 226Ra and Srnat found in this fraction were accounted for in the mass balance and interpretation of subsequent experimental results.  The subsequent leaching experiments were undertaken with the solid fraction containing associated Srnat and 226Ra.

# 2.4 	Aging of MBRR with associated strontium and radium

Samples of each equilibrated material were also sealed in air-tight containers as moist samples with a small amount (1–2 mL) of Milli-Q water added to keep them moist and placed in three temperature-controlled environments, at 4°, 23°, and 65°C, for a period of 6-months to determine effects of aging on the extent of sorption irreversibility.

# 2.5	Isotope exchange and leaching experiments

Isotope exchange experiments involved equilibration of the 226Ra- and Srnat-bearing MBRR solids (both freshly prepared solids and the solids aged at various temperatures) with aqueous tracer solutions (100 mL) containing known amounts of either 228Ra (~2.5 Bq/mL) or 85Sr (~5 Bq/mL).  The purpose of this step, which adds aqueous 228Ra and 85Sr to the systems containing MBRR, is to allow comparison of the sorption behaviour of the newly added tracer isotopes with the isotopes which had previously been added, equilibrated, and aged at different temperatures (226Ra and Srnat).  Any differences in behaviour of the isotopes of the same element can therefore be ascribed to irreversible phenomena or incorporation during the equilibration and aging steps.

To study the sorption of 228Ra and 85Sr as a function of pH, a sequential stepwise (stat) titration was carried out using a Metrohm Titrando autotitrator.  The MBRR solids were re-suspended with the appropriate 85Sr or 228Ra exchange solutions and transferred to a water-jacketed titration vessel maintained at 23°C.  The sample suspension was achieved by continuous stirring using an overhead propeller stirrer.  A sequential stepwise titration was performed for each sample, starting at a pH of 9 and finishing at pH 3.  The sequential stat titration maintains a constant pH for a specified time but provides a very sharp lowering of pH at the end of the holding period, such that a plot of pH against time appears as a series of flat steps.  The pH was lowered by one pH unit at each step, and maintained for one hour, after which a 2 mL sub-sample was collected and centrifuged through a 0.2 µm filter at 4500 rpm for 10 minutes.  The mass of the solid and liquid removed, and the volumes of acid added to adjust and maintain the pH at each step were continually tracked, enabling the mass balance of Ra and Sr isotopes to be monitored and determination of the partitioning co-efficient estimates (Kd) for the exchange isotopes (85Sr and 228Ra).  The latter is defined as the ratio of the concentration of adsorbed radionuclide in the solid (Bq/g) divided by the concentration in solution (Bq/mL) and has the units of mL/g.  Filtered supernatant was sub-sampled for subsequent analyses to quantify Srnat and other metals using Inductively Coupled Plasma Mass Spectrometry (ICP-MS), whereas the radioisotopes 85Sr, 226Ra and 228Ra, were determined by isotope-specific techniques (discussed in section 2.6).  Following the pH 3.0 sampling, the sample in the titration cell was left to stand overnight (16 hr). During this period the pH tended to drift upwards, and a second sub-sample was taken the following day after a 1 hr equilibration at pH 3.0.

2.6	Analysis

Samples from the Sr exchange experiments were measured by gamma-ray spectrometry to quantify the concentration of the 85Sr exchange isotope in solution.  This was followed by ICP-MS to quantify Srnat concentration (using the 88Sr signal).  85Sr was determined by counting samples for 1 hour using an ORTEC High Purity Germanium gamma-ray spectrometer, calibrated with a matrix and geometry matched 85Sr standard (prepared using Eckert & Ziegler 85Sr solution 1331-18-2).  The calculated counting efficiency was 5.6 % using the 514 keV 85Sr gamma-ray peak.  Strontium was quantified using an Agilent 4500 Quadrupole ICP-MS, as outlined in Clark et al. (2011).

Samples from the Ra exchange experiments underwent a complex chemical treatment where 226Ra was measured using alpha spectrometry and 228Ra was measured indirectly via its progeny 228Ac on a gas flow proportional counter.  Each sample solution was spiked with a GE Healthcare Ltd 133Ba yield radiotracer (source code S3/31/31) and purified according to Eichrom method RAW04 (Eichrom, 2014).  The pH of each sample solution was adjusted to pH 6-7 using NaOH and then passed through an Eichrom manganese dioxide resin column (MnO2 resin 100-200 mesh, MN-B100-A).  The Ra and Ba isotopes were retained on the column and then eluted, through dissolution of the MnO2 resin coating, with 5 M HCl-1.5 % H2O2.  The Ra/Ba solution was then equilibrated for >30 hours to allow for the ingrowth of the 228Ra progeny, 228Ac.  Equilibrated solutions were then passed through an Eichrom DGA resin cartridge (N,N,N’,N’-tetra-n-octyldiglycolamide - DGA Resin, Normal, 50-100 µm particle size, DN-R50-S) at which point Ra/Ba isotopes were eluted while 228Ac was retained; 228Ac was then eluted using 2 M HCl.

The Ra/Ba fractions were first counted for 10 minutes each on an ORTEC High Purity Germanium gamma-ray spectrometer, calibrated with a matrix- and geometry-matched 133Ba standard to establish the 133Ba radiotracer recovery and inferred recovery of the 226Ra and 228Ac.  An alpha source, prepared by precipitation with BaSO4 and collected on a 0.1 µm filter, was then counted for 48 hours on an alpha spectrometer, configured as described by Clark et al. (2011) to measure 226Ra.  The 228Ac fraction was precipitated with CeF3, collected on a 0.1 µm filter and counted on a Canberra Tennelec Series 5 XLB Gas-Flow Proportional Counter, calibrated with a matrix and geometry matched 90Sr/90Y beta standard.

Note that the reported data for exchange isotope (85Sr, 228Ra) recovered shown in the figures are expressed as a percentage of the known amount added.  Whereas, the reported data for the isotopes which are present in the aging experiments (and may also be present in the initial MBRR) are reported as a total activity (Bq/g of liquid) in the case of 226Ra or mass concentration (for Srnat).

3.	Results and Discussion

# 3.1	pH-dependent adsorption and desorption of Ra and Sr isotopes on non-aged MBRR samples

The experimental results for sorption of 228Ra and 85Sr, which were only present in the final isotope exchange step, show the short-term adsorption of these isotopes and the subsequent desorption as the pH was lowered.  The data for the percentage of 228Ra sorbed by the MBRR in the isotope exchange experiments (Fig. 1A) indicated that the MBRR materials removed ≥96 % of the 228Ra across a wide pH range (≈6 to 9). Below pH 6 there is a sharp sorption edge.  The strong initial adsorption of 228Ra demonstrates that the MBRR has a high affinity for Ra, as previously reported by Clark et al. (2011).  The sorption partitioning coefficient (Kd value) for 228Ra exceeds 1000 mL/g across a wide pH range ≈≥ 5; this decreases as the pH is reduced (Figure 1A).  It can also be seen in Figure 1A that there is little difference between 228Ra sorption behaviour for the two samples prepared at higher and lower loading concentrations of 226Ra.

Similarly, a high MBRR affinity for 85Sr was observed, however the binding of 85Sr was lower than the case of Ra across the near-neutral pH range (Fig. 2A).  The decrease in 85Sr binding as the pH is reduced was not as marked as for Ra, hence the pH edge has a reduced slope.  Kd values for 85Sr show a similar pH response, with values <100 mL/g for pH below about 6 (Fig. 2).  As with the radium case, the curves for the samples with different initial loadings of Srnat are quite similar.

The data for the release of 226Ra and Srnat from the MBRR samples during the pH stat experiments are shown in Figure 1B and 2B.  In Figure 1B, the y axis shows the amount of 226Ra released from the solid as a function of pH.  The 226Ra associated with the solid is strongly bound and remains associated mainly with the solid as the pH is lowered from 9 to 6, but below this pH significant amounts are released to solution.  A clear distinction between the behaviour of the samples loaded with different amounts of 226Ra is observed (Fig 1B).  This reflects the greater available accessible pool in the experiments with the higher 226Ra loading.  While this feature is not surprising, it underlines the ability of the techniques to discriminate samples containing differing amounts of accessible radionuclides.

The desorption behaviour of the Srnat shows a similar pattern (Fig 2B), and again the displacement of the two curves reflects the different loading conditions of the experiments in terms of the added Srnat concentrations.  The curves in Figure 2B clearly show that the Srnat is strongly bound by the solid at the initial high pH values and progressively comes into solution as the pH is lowered.  However, there is a slight difference to the Ra case, in that the measured concentrations of Srnat in solution include a significant baseline contribution from the inherent Srnat content of the MBRR.  For this reason, the Sr in solution for the higher concentration experiments is not proportional to the Srnat added during the pre-equilibration step.  Thus, the curves in the two experiments (Fig 2B) are somewhat closer to each other than for Figure 1B.  Hence, if the higher concentration provides twice the soluble concentration as the lower concentration (as for Ra) then the background supply can be estimated (Fig 2B).

The raw sorption and leaching data presented in Figure 1 and 2 provide useful information on the behaviour of the system. There are some significant aspects of the data for these exchange experiments and the relationship between the concentrations of the isotope pairs, and the effect of different aging conditions, is discussed in more detail below.

B

A

Figure 1. Aqueous percentage of 228Ra (Panel A) in solution and sorption Kd values measured during sequential stat titrations for samples with low (L: 5 x 10-11 M) and high (H: 1 x 10-10 M) initial loadings of (natural) 226Ra. Panel B shows the release of 226Ra into solution as the pH was lowered, with experiments with low and higher added Ra compared. Comparison of the two curves shows the effect of the additional Ra incrementing concentrations in the solution phase.

A

B

Figure 2.  Strontium data collected showing aqueous concentrations of 85Sr (tracer) and Srnat in solution as measured during sequential stat titrations.  Figure 2A shows proportion sorbed and Kd data for 85Sr for experiments at low (L: 1.14 x 10-5 M) and high (H: 2.34 x 10-5 M) initial loadings of added stable Srnat, respectively. Figure 2B shows the release of Srnat into solution as the pH was lowered, in experiments with both low and higher added Srnat. Comparison of the two curves shows the effect of the additional Sr incrementing concentrations in the solution phase.  Both experiments depicted in 2B also contain additional (background) Srnat derived from the MBRR, which is estimated mathematically.

The aqueous chemistry of the radionuclides should be considered in interpreting their uptake/sorption behaviour.  Radium has a pH-dependent speciation, particularly with carbonate and sulfate, with Ra2+ and RaSO4(aq) dominant at pH 4, RaHCO3+ dominant from pH 6 to 8 and RaCO3(aq) becomes dominant at pH 10 (Baeza et al., 2006; Van Beek et al., 2004).  Radium hydroxide is also the most soluble of the alkaline earth hydroxides (Kirby and Salutsky, 1964) (therefore must have a Ksp greater than the Ksp for Ba(OH)2 (2.55x10-4), (Lide, 2003)) and is unlikely to precipitate directly.  In addition, RaCO3, is about an order of magnitude more soluble than BaCO3 (Kirby and Salutsky, 1964) giving a Ksp of 1.86x10-8 (Matyskin, 2016) compared to the Ksp of BaCO3 (2.55x10-9), and SrCO3 (5.36x10-10 (Lide, 2003)).  However, substantial alkalinity is available in the MBRR, which at high pH, where most Ra retention occurs, suggests that alkalinity will be present as carbonates (Stumm and Morgan, 1996a).  By using the Ksp estimates of 1.86x10-8 for RaCO3 and 5.36x10-10 for SrCO3 (with 250 mg/L CaCO3 alkalinity) geochemical modelling suggests that Ra could be removed to concentrations of about 1.36x10-4 M Ra and Sr to about 2.32x10-5 M.  These solubility estimates for Ra concentrations from carbonate precipitation exceed the concentrations used in our experiments by some four orders of magnitude, but the Sr concentrations are such that solutions may become saturated for SrCO3 at 2.33 x 10-5 M.  Hence, direct carbonate precipitation is possible at elevated alkalinity (≈250 mg/L CaCO3 equivalent) for the initial Sr added, but not for the Ra; for Ra, other mechanisms (apart from precipitation) must be considered for removal.

Clark et al. (2011), suggest that Ra removal to MBRR can be attributed to co-precipitation of the hydrotalcite (Mg6Al2(CO3)(OH)16•4H2O), which provides much lower possible Ra concentrations than simple hydroxide and/or carbonate precipitation. Strontium has similar mineralogy to Mg, forming strontiodresserite ((Sr,Ca)Al2(CO3)2(OH)4•H2O) (a Ca, Sr correlative of dresserite (BaAl2(CO3)2(OH)4•H2O)), which may act to remove Sr to low concentrations; waste Sr removal to hydrotalcite has been shown to be effective.  Furthermore, coupled dissolution-reprecipitation may readily occur at concentrations well below saturation conditions (Di Lorenzo et al., 2018; Hövelmann et al., 2018; Ruiz-Agudo et al., 2014; Ruiz-Agudo et al., 2017), particularly at or near cleavage surfaces (Ruiz-Agudo et al., 2014; Ruiz-Agudo et al., 2017). Hence, although complete Ra removal by barite co-precipitation is well known, Ra has been shown to barely (if at all) substitute in (simple) Sr minerals, which by consequence reduces the possible substitution into (much smaller) Ca or Mg sites.  Also, Ca-hydroxy-carbonates, such as hydrocalumite and para-hydroxycarbonate among others, are more likely to revert into simple carbonate and hydroxide minerals in seawater neutralised residues compared to Mg correlatives (Palmer et al., 2011a; Palmer et al., 2011b). Hence, coupled dissolution-reprecipitation (Di Lorenzo et al., 2018; Hövelmann et al., 2018; Ruiz-Agudo et al., 2014; Ruiz-Agudo et al., 2017) may readily occur around the hydrocalumite and para-hydroxycarbonate mineral suites because of the reversion instability and consequently, Ra removal by coupled dissolution-reprecipitation into pre-existing hydroxyl-carbonate may well help partially explain the very efficient removals of Ra observed by Clark et al (2011), and the binding observed here.

In addition, several previous studies also suggest that Ra adsorption by iron oxide is of significance (Burghardt and Kassahun, 2005; Nikolaou and Lekkas, 2001; Sasaki et al., 2008; Vaaramaa et al., 2003), especially when dissolved species are mostly un-charged (Baeza et al., 2006; Degremont, 1979).  The sorption data presented in Figures 1 and 2 are consistent with higher removal efficiencies at higher pH reported in the literature.  The pH dependence of cation adsorption is observed for all oxides and originates from the amphoteric properties of surface hydroxyl sites (Bassot et al., 2001; Chau and Kopeć, 2010; Dzombak and Morel, 1990; Vaaramaa et al., 2003).  More specifically, this behaviour is thought to occur at higher pH (>7.5) where there is effective colloidal particle charge neutralisation (Baeza et al., 2006; Degremont, 1979; Shao et al., 2009), which is observed in the reaction vessels.  Given that the geochemistry of Sr is very similar to Ra and Ca (Rihs et al., 2000; Schmidt and Cochran, 2010; Van Beek et al., 2004), then mechanisms implicated for one element are likely to apply to the other.  Indeed, several studies (e.g., (Axe et al., 1998; Axe and Trivedi, 2002; Hofmann et al., 2005; Trivedi and Axe, 1999) indicate the strong association of Sr with Fe-, Al-, and Mn-oxyhydroxides.  Hence, the data presented are consistent with high removal efficiencies at higher pH reported in the literature (Figs. 1 & 2).

The adsorption and desorption behaviour of Ra and Sr in these experiments can be related to the dissolution and reactivity of mineral phases comprising the MBRR inferred from elemental analyses. Solution analysis of other major elements (Fig. 3) from the sequential stat titration extracts indicates that Ca, Na, and Mg show relatively steady rises in concentration as pH is lowered.  At the lower experimental pH values (pH 3 and 3 overnight) for Na, there appears to be a plateauing of the data, suggesting that Na sources within the MBRR mineralogy are exhausted (Fig. 3B).  In addition, Mg appears to show an increased rate of supply to the solution at pH <5, similar to Fe (Fig. 3A).  Consequently, when viewed on a linear scale (Fig. 3B), there is increased Mg availability at pH <5, which is more strongly emphasised at pH 4 and again at pH 3.  However, 226Ra release from the solids (Fig. 1B) most closely follows the release of Al (Fig. 3B), which may arise from the dissolution of gibbsite, hydrotalcites, and/or hydrocalumites known to be present in MBRR.  As such the dissolution of these phases would release associated bound 226Ra.

B

A

Figure 3. Mean element concentrations released from the MBRRs (A: logarithmic scale for contrast of major and minor metals; B: linear scale for major metals) during titration from pH 9 to 3 and after equilibration at pH 3 overnight. Sodium data have been corrected to remove the contribution from the reaction solution (0.01 M NaNO3).

Clark et al. (2011) showed, using thermodynamic geochemical modelling, that most MBRRs have an over saturation of Ca- and Mg-carbonates, including, and particularly, hydrotalcite.  These results indicated they are also in kinetic disequilibrium with their sampled waters because saturation indices are > 0.  However, Clark et al. (2011) showed that it is not until the model-pH is allowed to rise to pH 12 (some 27 times the original model’s alkalinity) that Ra adsorption as =FeO-Ra-OH becomes significant. Once adsorption becomes significant, adsorption involves a positively charged species (eg, RaOH+) rather than neutral species (Baeza et al., 2006; Degremont, 1979).  Moreover, Clark et al. (2011) indicated that gibbsite Al(OH)3 has little involvement with Ra removal, and that in their geochemical models, groundwaters have insufficient Ra in solution for direct Ra-precipitation as either carbonates, sulphates, or hydroxides. Therefore, if Ra precipitation is occurring, then it must be occurring as a co-precipitate within one or more over-saturated mineral phases; most likely hydrotalcite-like minerals.  Many authors (e.g., (Couperthwaite et al., 2013; Das et al., 2002; El Shafei, 2002; Robertson et al., 2016; Rozov et al., 2011) show that hydrotalcite-like minerals can accept both cations and anions within their structures, which provides thermodynamic and geochemical stability.  Moreover, Couperthwaite et al. (2013) demonstrated that hydrotalcite is very stable under acidic conditions to pH 5.5, where it then starts to react to neutralise acid and release bound trace elements.  A pH of 5.5 is also coincidental with the increased solubility of Al from gibbsite (Al(OH)3) (Stumm and Morgan, 1996b).  Consequently, it is difficult to determine if the Sr and Ra releases, which are coincidental with an Al release to the solution, arise from the dissolution of alumina-bound materials, from dissolution of substituted hydrotalcite-like precipitates at pH ≤ 5, or both.

3.2	pH-dependent adsorption and desorption of Ra and Sr isotopes on MBRR samples aged at various temperatures

The binding behaviours of newly added 228Ra to pre-loaded MBRR’s aged at three different temperatures are compared to the unaged sample in Figure 4A.  These curves show the extent of sorption on the sample, depicting the short-term 228Ra binding by the solid (i.e., during the stat-titration exchange experiment).  The 228Ra-binding properties of the solids exhibit a similar pH dependence and near-total binding in the neutral pH ranges.  Aging the sample at 4°C did not greatly change the 228Ra sorption behaviour, however the 228Ra binding in samples aged at the higher temperatures is slightly stronger (Fig. 4A).  This suggests that small changes to the surface chemistry occurred during sample aging, leading to changed sorption properties.  Figure 4B shows the release of 226Ra, and in this case, the data show that the 65°C aged sample exhibits a greater binding of 226Ra by the solid.  Therefore, Figure 4B indicates that binding of 226Ra has been altered somewhat by the aging, particularly at elevated temperatures.

B

A

Figure 4. Comparison of newly added 228Ra binding by the solid (A) with the desorption behaviour of previously bound 226Ra (B). Experiments are with samples loaded with 1 x 10-10 M of Ra.  Data are represented as the total amount of each isotope in solution (fraction of added 228Ra in solution or total 226Ra in solution (Bq/g of liquid)).

The uptake and release data for Sr isotopes are somewhat different from that for Ra (Figs. 5 & 6).  In this case, the newly added 85Sr is more strongly bound by the aged solids in the pH range from 9 to 6 (compared to the unaged solid) although the different curves tend to converge at lower pH.  Again, this suggests slight changes in the sorption properties (in this case for Sr) resulting from aging, possibly by the formation or alteration of mineral phases.  However, it is clear from Figures 5B and 6B that the distribution of Srnat is significantly altered by the aging step, with significantly stronger binding by all the aged samples across the entire pH range. In particular, the significant difference between the curves for the aged samples and the unaged sample (Figs. 5B & 6B) continue into the low pH range. The Srnat release from all 3 aged samples as the pH reduces is significantly less than the unaged sample. This shows that during aging, some Srnat has been incorporated in inaccessible phases.  Also, the Srnat retention properties of the aged solid differ slightly, with the aged samples releasing further bound Srnat with the overnight aging at pH 3 (Figs. 5B & 6B). In contrast there is no significant release of Srnat from the unaged sample during this time.

A

B

Figure 5. Comparison of newly added 85Sr binding by the solid (A) with the desorption behaviour of previously bound stable strontium (B). Experiments with 1.14 x 10-5 M of strontium.  Data are represented as total amount of each isotope in solution (proportion of added 85Sr in solution or total stable strontium in solution (mg/L)).

A

B

Figure 6. Comparison of newly added 85Sr binding by the solid (A) with the desorption behaviour of previously bound stable strontium (B). Experiments with 2.34 x 10-5 M of strontium.  Data are represented as total amount of each isotope in solution (proportion of added 85Sr in solution or total stable strontium in solution (mg/L)).

The results for both Ra and Sr aging experiments show the importance of distinguishing between the effects caused by changed surface properties of the solid during aging from effects caused by incorporation during aging.  There are literature examples of both scenarios in other systems.  For example, Payne et al. (1994) reported the effect of aging on U uptake by iron oxides.  In that case, the sorption of U on the aged solid was weaker than the unaged, and some uranium was incorporated during the aging step.  In the current example of Ra sorption on MBRR, the effect of aging is to slightly increase (e.g. (Clark et al., 2015) the sorptive properties of the solid.  However, the behaviour of Srnat was somewhat similar to that reported by Payne et al (1994) in the U-Fe-oxide case, with evidence for some incorporation of Sr during aging.

# 3.3 Isotopic Exchange plots

Although the adsorption/desorption experiments suggest that there is a stronger fast sorption binding of 228Ra by aged samples (than unaged) particularly when aged at the higher temperature (Fig. 4B), the isotopic exchange plots for Ra data (% 226Ra against 228Ra; Fig. 7) suggest that aging has little effect on the irreversible binding (i.e. there has been limited incorporation of 226Ra in the solid during aging).  If such incorporation were occurring, it would be expected that fitted lines for the aged samples in Figure 7 would have been displaced from the unaged sample, which was not observed.  In contrast, the comparison of Figure 7A and 7B shows that the only major difference between the two sets of experiments is attributable to the different amounts of 226Ra present during the aging step (demonstrated primarily by the y intercepts).  In other words, increasing the 226Ra concentration for initial adsorption increased the amount of bound 226Ra (Fig. 7A), but the aging temperature had no significant effect.  However, when data are recalculated as a proportion of the initial 226Ra concentration (Figs. 7C & 7D), very similar proportions of 226Ra are irreversibly bound; this calculation indicates that ≈60 % of 226Ra is irreversibly bound.  These data suggest that 226Ra availability and release from MBRR is primarily controlled by sorption equilibria.  As previously noted, aging appears to cause recrystallisation of a phase having different sorption properties for 228Ra, but there is limited diffusion and/or incorporation of 226Ra into existing or newly formed solid phases.

B

A

D

C

Figure 7 Low concentration (A) and high concentration (B) Ra isotopic exchange plots for unaged (blue squares) and materials aged at 4°C (red circles), 25°C (green triangles), and 65°C (purple diamonds), show that aging has little or no effect on 226Ra release by the 228Ra exchange isotope.  Figures 7C & D show the data in Figures 7A & B reprocessed with irreversibly bound proportion estimates made for 228Ra initially added.

The situation in the case of Sr is somewhat different (Figs. 8 & 9). Both figures show that there is an increase of Srnat binding by the solid due to aging at both concentrations.  The isotopic exchange plots show about a 20 % increase in retention of Srnat with aging (Fig. 8) and aging at 25°C and 65°C result in greater binding than 4°C (Figs. 5, 6 & 8).  However, in the standard isotopic exchange plots (Fig. 8) the Srnat data sets appears to exhibit a change in slope (circled; Figs. 8A & 8B), this change in slope is coincidental with the pH 6 to 5 transition observed in the analogous uptake curves and the associated release of Al from the solid (Figs. 3 & 4).  The greatest deviation from linearity in Figure 8 is exhibited in the three aged samples, suggesting that the effect is a product of the aging process.  It appears that the observed changes in slope reflect the changes in available Srnat pools and the possible dissolution of metastable mineral phases which become dissolved as the pH is reduced; this can be seen by comparison with Figure 3 where the amount of Al in solution is much greater below pH 5.

When isotopic exchange data for Srnat are considered separately for the different pH ranges (pH ≥5 and pH ≤5) there is a clear indication that aging has had an effect on the distribution of prior bound Srnat (Fig. 9).  There are clear increases in Srnat retention from pH 9 to 6 (heavy correlation lines; Figs. 9A and 9B), whereas there is systematic reduction in availability of Srnat by about 40 % from unaged material to materials aged at 65°C for both concentrations.  At pH ≤6 the supply of the pre-existing Srnat pools generates a complex pattern.  Consequently, plotting the isotope exchange data in the range pH ≥5 separates the effects of mobilisation and release of the pre-existing Srnat pool indicating that some 4.7 mg/L (or 23.5 %) of the newly added Srnat at high concentration becomes available; this available Srnat decreases with aging for all temperatures.  This, therefore, allows the recalculation of data as a proportion of the Srnat (Figs. 9C & 9D) which appear to be ≈68 % irreversible for the initial low loadings and ≈76 % for the initial high loadings.  Aging at 65°C indicates only about 1.8 mg/L (18 %) of the newly added Srnat is released for low concentration additions (Figs. 9A & 9C), and only about 2.8 mg (24 %) is available from the higher concentration (Figs. 9B & 9D).  In summary, the changes in slope of Figure 9A and 9B are most likely from the dissolution of a metastable Sr bearing phase(s) around pH 5 (Fig. 3).  Following the dissolution of this phase, below this pH the released Sr participates in adsorption-desorption reactions.

B

A

Fig 8 Low concentration Sr isotopic exchange data (A) and high concentration Sr isotopic exchange data (B); blue square = initial loadings; red circle = 4°C aging; green triangle = 25°C aging, purple diamond = 65°C aging.  Although good linear data fits can be applied, the circled data appear to be inflection points for each temperature, and are at pH 5 or 6, when pre-existing Srnat from the seawater neutralisation begin to be included in the Srnat data.

B

A

D

C

Figure 9. Sr isotopic exchange data for (A) low concentration and (B) high concentrations of added Srnat.  with a separation on pH ≥ 5 and pH ≤ 5 data; square = initial loadings; circle = 4°C aging; triangle = 25°C aging, diamond = 65°C aging.  Linear correlations for pH ≥ 5 are forced through zero and are plotted as heavy solid lines and symbols, pH ≤ 5 data are linear correlated without forcing and are plotted as ghosted thin lines, and open symbols. Figures 9 C and D are pH ≥5 data only with irreversibly bound proportion estimates where pre-existing Sr contributions are minimised. However, because the pre-existing Sr contributions are unknown, the irreversibility estimates are minimums and are more likely to be influential in low loading concentration data (Figure 9C).

The differences in isotopic exchange behaviour between 226Ra and Srnat (Figs. 7 & 9), suggest that Srnat has been redistributed to new irreversible binding sites across possibly multiple mineral phases, whereas the 226Ra was transferred only to kinetically less favourable sites, but that these sites remain reversible.  Such kinetically less favourable sites that remain reversible are most likely representative of a phase recrystallisation, such as the hydrotalcite phases suggested by (Clark et al., 2015).

The redistribution of Srnat during aging (Figs. 8 & 9, but particularly pH ≥ 5 data; Fig. 9) suggests that a redistribution occurs from Sr-containing Ca-hydroxy-carbonates, such as hydrocalumite and para-hydroxycarbonate, which are more likely to revert into simple carbonate and hydroxides as indicated by Palmer et al. (2011a); (2011b).  Moreover, Fe, Al and Mn oxides have all been shown to not only surface-sorb Sr, but to also allow diffusion of Sr through and within defect sites, particular within nano-pores of 2-5 nm (Axe and Anderson, 1997; Axe and Trivedi, 2002; Hofmann et al., 2005; Trivedi and Axe, 1999, 2001); the inter particular diffusion rate is typically controlled by pH and the activation energy required to break the site binding energy.  Given that the greatest occlusion of Sr is seen at 65°C aging, these data are consistent with an activation energy threshold for Sr distribution, and suggestive that oxide diffusion particularly within Fe- and/or Al-oxyhydroxides is occurring for Srnat (Fig. 9), but not for 226Ra (Fig. 7).

# Conclusions

The isotope exchange techniques have considerable value in elucidating the mechanism of rapid adsorption and desorption of Ra and Sr to the MBRR materials, as well as the incorporation of Ra and Sr during the aging of the materials. The data presented here indicate that:

- Both Ra and Sr are readily bound to MBRR materials;

- Both Ra and Sr are most stably bound at pH ≥6;

- The release of both Sr and Ra from the MBRR appear to be controlled in part by dissolution of the hydrotalcite minerals generated during BRR modification with seawater;

- The aging temperature of 226Ra associated with MBRR has little or no effect on its subsequent availability (Figs. 4 & 7), but does appear to alter the surface sorption properties for Ra, suggesting recrystallisation of a single phase that is soluble at low pH (e.g., hydrotalcites);

- The Srnat data are heavily influenced by the aging of the pool of Srnat in the MBRR, which becomes available at pH ≤ 6 and influences the isotopic exchange plots (Figs. 8 & 9) as well as contributing to the amount of Sr leached from the solid (Fig. 2B);

- The aging of MBRR samples with added Srnat shows redistribution to multiple phases with irreversible binding sites, suggesting diffusion within Fe- and/or Al-oxyhydroxides.

The data show the value of isotope exchange methods in this type of work by highlighting the different behaviour of Srnat and 226Ra during aging, as well as the different adsorption properties of the aged samples (particularly for Ra).  The experiments were particularly useful for identifying sorption properties and the incorporation and mechanisms of metal release from the solids. During the course of the aging period, a substantial proportion of the added Sr was incorporated into inaccessible phases, possibly via inclusion into Fe- and/or Al-oxyhydroxides.  However, 226Ra appears to only have been re-distributed to a limited extent.  Hence, MBRR materials can facilitate remediation and long-term storage for both Sr and Ra, where aging has the potential to further reduce metal accessibility and resistance to leaching, particularly for Sr.

# Acknowledgments

We would like to thank AINSE for the provision of AINSE Grant AINGRA10036 that allowed the completion of this work, particularly the large number of samples for counting.

# References

Axe, L., Anderson, P.R., 1997. Experimental and Theoretical Diffusivities of Cd and Sr in Hydrous Ferric Oxide. J Colloid Interface Sci 185, 436-448.

Axe, L., Bunker, G.B., Anderson, P.R., Tyson, T.A., 1998. An XAFS Analysis of Strontium at the Hydrous Ferric Oxide Surface. Journal of Colloid and Interface Science 199, 44-52.

Axe, L., Trivedi, P., 2002. Intraparticle surface diffusion of metal contaminants and their attenuation in microporous amorphous Al, Fe, and Mn oxides. Journal of Colloid and Interface Science 247, 259-265.

Baeza, A., Del Rio, L.M., Jimenez, A., Miro, C., Paniagua, J.M., 1995. Factors determining the radioactivity levels of waters in the province of Caceres (Spain). Appl Radiat Isot 46, 1053-1059.

Baeza, A., Fernandez, M., Herranz, M., Legarda, F., Miro, C., A., S., 2006. Removing uranium and radium from a natural water. Water, Air, and Soil Pollution 173, 57-69.

Bassot, S., Mallot, C., Stammose, D., 2001. Experimental study and modeling of the radium isotope onto goethite. Materials Research Society Symposium Procceedings 663, 1081-1089.

Burghardt, D., Kassahun, A., 2005. Development of a reactive zone technology for simultaneous in situ immobilisation of radium and uranium. Environ. Geol. 49, 314-320.

Chau, N.D., Kopeć, M., 2010. Factors controlling concentrations and activity ratios of radium isotopes in groundwaters. Przeglad Geologiczny 58, 499-505.

Chiang, P.N., Wang, M.K., Huang, P.M., Wang, J.J., Chiu, C.Y., 2010. Cesium and strontium sorption by selected tropical and subtropical soils around nuclear facilities. Journal of Environmental Radioactivity 101, 472-481.

Clark, M., Berry, J., McConchie, D., 2009. The long-term stability of a metal-laden BauxsolTM reagent under different geochemical conditions. Geochem: Explor: Environ: Anal 9, 101-112.

Clark, M.W., Akhurst, D.J., Fergusson, L., 2011. Removal of radium from groundwater using a modified bauxite refinery residue. J. Environ. Qual. 40, 1835-1843.

Clark, M.W., Payne, T.E., Harrison, J.J., Comarmond, M.J., Collins, R.N., Reichelt-Brushett, A.J., 2015. Reversibility of uranium and thorium binding on a modified bauxite refinery residue: The effects of aging temperature. Applied Geochemistry 53, 79-90.

Collins, R.N., Clark, M.W., Payne, T.E., 2014. Solid phases responsible for MnII, CrIII, CoII, Ni, CuII and Zn immobilization by a modified bauxite refinery residue (red mud) at pH 7.5. Chemical Engineering Journal 236, 419-429.

Couperthwaite, S.J., Han, S., Santini, T., Kaur, G., Johnstone, D.W., Millar, G.J., Frost, R.L., 2013. Bauxite residue neutralisation precipitate stability in acidic environments. Enviro. Chem. 10, 455-464.

Das, J., Das, D., Dash, G.P., Parida, K.M., 2002. Studies on Mg/Fe hydrotalcite-like-compound (HTlc): I. Removal of inorganic selenite (SeO3 2-) from aqueous medium. Journal of Colloid and Interface Science 251, 26-32.

Degremont, 1979. Manual tecnic del agua, in: Grafo, S.A. (Ed.), CEDEX. Bilbao, Rueli-Malmaison, France, pp. 135-143.

Di Lorenzo, F., Ruiz-Agudo, C., IbaĂąez-Velasco, A., Gil-San MillĂĄn, R., Navarro, J.A.R., Ruiz-Agudo, E., Rodriguez-Navarro, C., 2018. The carbonation of wollastonite: A model reaction to test natural and biomimetic catalysts for enhanced CO2 sequestration. Minerals 8.

Dzombak, D.A., Morel, F.M.M., 1990. Surface Complexation Modeling:  Hydrous Ferric Oxide. Wiley-Interscience Publication, New York.

El Shafei, G.M.S., 2002. Change of structural and adsorption properties due to isomorphous substitution in hydrotalcite-like materials. Adsorption Sci. Technol. 20, 767-786.

Eichrom, 2014. Method RAW04 Revision 1.1 Radium-226/228 In Water (MnO2 Resin and DGA Resin, Eichrom Technologies, LLC, 9pp

Genç-Fuhrman, H., 2004. Arsenic removal from water using seawater-neutralised red-mud (Bauxsol), Environment and Resources. Technical University of Denmark, Copenhagen.

Hofmann, A., Van Beinum, W., Meeussen, J.C.L., Kretzschmar, R., 2005. Sorption kinetics of strontium in porous hydrous ferric oxide aggregates II. Comparison of experimental results and model predictions. Journal of Colloid and Interface Science 283, 29-40.

Hövelmann, J., Putnis, C.V., Benning, L.G., 2018. Metal sequestration through coupled dissolutionâ“ precipitation at the Brucite “Water interface. Minerals 8.

Kirby, H.W., Salutsky, M.L., 1964. The Radiochemistry of Radium, Nuclear Science Series, National Academy of Science-National Research Council Series US Atomic Energy Commission, Sprinfield Virginia, p. 205.

Lapointe, F., Fytas, K., McConchie, D., 2006. Efficiency of Bauxsol™ in permeable reactive barriers to treat acid rock drainage. Mine Wat. Enviro. 25, 37-44.

Lide, D.R., 2003. Handbook of Chemistry and Physics, 84th Edition ed. CRC Press, Boca Raton, p. 2553.

Matyskin, A.V., 2016. On the solubility of radium sulfate and carbonate. Thesis For The Degree Of Licentiate Of Engineering, Chalmers University Of Technology, Gothenburg, Sweden, 45pp

Mays, C.W., 1988. Alpha-particle-induced cancer in humans. Health Physics 55, 637-652.

Mays, C.W., Rowland, R.E., Stehney, R.F., 1985. Cancer risk from the lifetime intake of Ra and U isotopes. Health Physics 48, 635-647.

McConchie, D., Clark, M., Davies-McConchie, F., 2001. Processes and Compositions for Water Treatment. Neauveau Technology Investments, Australian, p. 28.

McConchie, D., Clark, M., Hanahan, C., Fawkes, R., 1999. The use of seawater-neutralised bauxite refinery residues (red mud) in environmental remediation programs, in: Gaballah, I., Hager, J., Solozabal, R. (Eds.), Global Symposium on Recycling, Waste Treatment and Clean Technology (REWAS 1999), San Sebastian, pp. 391-400.

Milvy, P., Cothern, C.R., 1990. Scientific Background for the Development of Regulations for. Radionuclides in Drinking Water in: C. R. Cothern, Reberts, P.A. (Eds.), Radon, Radium and Uranium in Drinking Water. Lewis Publishers, Chelsea, Michigan, pp. 1-16.

Nikolaou, A.D., Lekkas, T.D., 2001. In-situ treatment of radioactive mine water using reactive materials - Results of laboratory and field experiments in uranium ore mines in Germany. Acta Hydrochimica et Hydrobiologica 29, 129-138.

Palmer, S.J., Frost, R.L., 2010. Use of hydrotalcites for the removal of toxic anions from aqueous solutions. Industrial and Engineering Chemistry Research 49, 8969-8976.

Palmer, S.J., Frost, R.L., Smith, M.K., 2011a. Minimising reversion, using seawater and magnesium chloride, caused by the dissolution of tricalcium aluminate hexahydrate. J Colloid Interface Sci 353, 398-405.

Palmer, S.J., Grand, L.M., Frost, R.L., 2010. Thermal analysis of hydrotalcite synthesised from aluminate solutions. Journal of Thermal Analysis and Calorimetry, 1-6.

Palmer, S.J., Smith, M.K., Frost, R.L., 2011b. The effect of high concentrations of calcium hydroxide in neutralised synthetic supernatant liquor-Implications for alumina refinery residues. Journal of Industrial and Engineering Chemistry 17, 56-61.

Payne, T.E., Davis, J.A. and Waite, T.D. (1994). Uranium Retention by Weathered Schists - The Role of Iron Minerals. Radiochimica Acta 66/67: 297-303.

Payne, T.E., Hatje, V., Itakura, T., McOrist, G.D. and Russell, R. (2004) Radionuclide applications in laboratory studies of environmental surface reactions. Journal of Environmental Radioactivity 76, 237-251.

Raabe, O.G., Book, S.A., Parks, N.J., 1983. Lifetime bone cancer dose-response relationships in beagles and people from skeletal burdens of 226Ra and 90Sr. Health Physics 44, 33-48.

Rachkova, N.G., Shuktomova, I.I., Taskaev, A.I., 2010. The state of natural radionuclides of uranium, radium, and thorium in soils. Eurasian Soil Science 43, 651-658.

Rihs, S., Condomines, M., Sigmarsson, O., 2000. U, Ra and Ba incorporation during precipitation of hydrothermal carbonates: Implications for 226Ra-Ba dating of impure travertines. Geochim. Cosmochim. Acta 64, 661-671.

Robertson, J., Hendry, M.J., Essilfie-Dughan, J., Chen, J., 2016. Precipitation of aluminum and magnesium secondary minerals from uranium mill raffinate (pH 1.0-10.5) and their controls on aqueous contaminants. Applied Geochemistry 64, 30-42.

Rozov, K.B., Berner, U., Kulik, D.A., Diamond, L.W., 2011. Solubility and thermodynamic properties of carbonate-bearing hydrotalcite-pyroaurite solid solutions with a 3:1 Mg/(Al+Fe) mole ratio. Clays and Clay Minerals 59, 215-232.

Ruiz-Agudo, E., Putnis, C.V., Putnis, A., 2014. Coupled dissolution and precipitation at mineral-fluid interfaces. Chem. Geol. 383, 132-146.

Ruiz-Agudo, E., Putnis, C.V., RodrĂ­guez-Navarro, C., 2017. Reactions between minerals and aqueous solutions, European Mineralogical Union Notes in Mineralogy. Mineralogical Society, pp. 419-467.

Sasaki, T., Gunji, Y., Iida, T., 2008. Theoretical basis for measuring small radon diffusion coefficients for a radium-bearing porous material generated by precipitation of iron (III) hydroxide. J. Nuclear Sci. and Technol. 45, 647-652.

Schmidt, S., Cochran, J.K., 2010. Radium and radium-daughter nuclides in carbonates: A brief overview of strategies for determining chronologies. Journal of Environmental Radioactivity 101, 530-537.

Shao, H., Dmytrieva, S.V., Kolditz, O., Kulik, D.A., Pfingsten, W., Kosakowski, G., 2009. Modeling reactive transport in non-ideal aqueous-solid solution system. Applied Geochemistry 24, 1287-1300.

Steinhauser, G., Niisoe, T., Harada, K.H., Shozugawa, K., Schneider, S., Synal, H.A., Walther, C., Christl, M., Nanba, K., Ishikawa, H., Koizumi, A., 2015. Post-Accident Sporadic Releases of Airborne Radionuclides from the Fukushima Daiichi Nuclear Power Plant Site. Environ. Sci. Technol. 49, 14028-14035.

Stumm, W., Morgan, J.J., 1996a. Aquatic Chemistry, 3 ed. John Wiley & Sons, New York.

Stumm, W., Morgan, J.J., 1996b. Aquatic Chemistry - Chemical Equilibria and Rates in Natural Waters -3rd ed. Wiley-Interscience, New York.

Sturchio, N.C., Banner, J.L., Binz, C.M., Heraty, L.B., Musgrove, M., 2001. Radium geochemistry of ground waters in Paleozoic carbonate aquifers, midcontinent, USA. Applied Geochemistry 16, 109-122.

Thiry, Y., Van Hees, M., 2008. Evolution of pH, organic matter and 226radium/calcium partitioning in U-mining debris following revegetation with pine trees. Sci. Tot. Environ. 393, 111-117.

Tracy, B.L., Prantl, F.A., 1983. 25 years of fission product input to Lakes Superior and Huron. Water, Air, and Soil Pollution 19, 15-27.

Trivedi, P., Axe, L., 1999. A comparison of strontium sorption to hydrous aluminum, iron, and manganese oxides. Journal of Colloid and Interface Science 218, 554-563.

Trivedi, P., Axe, L., 2001. Predicting divalent metal sorption to hydrous Al, Fe, and Mn oxides. Environ. Sci. Technol. 35, 1779-1784.

USEPA, 1976. National primary drinking-water regulations. Office of Water Supply, Washington, DC.

USEPA, 1996. Drinking water regulations and health advisories. Office of Water Supply, Washington, DC.

Vaaramaa, K., Lehto, J., Ervanne, H., 2003. Soluble and particle-bound 234,238U, 226Ra and 210Po in ground waters. Radiochim. Acta 91, 21-27.

Van Beek, P., Reyss, J.L., Demaster, D., Paterne, M., 2004. 226Ra-in marine barite: Relationship with carbonate dissolution and sediment focusing in the equatorial pacific. Deep-Sea Research Part I: Oceanographic Research Papers 51, 235-261.

Yoshida, Y., Yoshikawa, H., 2009. Estimation of Ra concentration in high-level radioactive waste disposal system, Materials Research Society Symposium Proceedings, Boston, MA, pp. 413-420.

Zawadzki, A., Cook, M., Cutmore, B., Evans, F., Fierro, D., Gedz, A., Harrison, J.J., Loosz, T., Medley, P., Mokhber-Shahin, L., Mullins, S., Sdraulig, S., 2017. Comparison of radium-228 determination in water among Australian laboratories. Journal of Environmental Radioactivity 178-179, 411-418.