Supporting Information

Modulating the Isotopic Hydrogen-Deuterium Exchange in Functionalized Nanocellulose to optimize SANS contrast

Vikram Singh Raghuwanshi1,*, David Joram Mendoza1, Jitendra Mata 2, 3, Gil Garnier1,*

1Bioresource Processing Research Institute of Australia (BioPRIA), Department of Chemical and Biological Engineering, Monash University, Clayton, Victoria-3800, Australia.

2Australian Centre for Neutron Scattering (ACNS), Australian Nuclear Science and Technology Organisation (ANSTO), Lucas Height, New South Wales-2234, Australia.

3School of Chemistry, University of New South Wales, NSW, Australia.

*Email: gil.garnier@monash.edu

vikram.raghuwanshi@monash.edu

S1: Calculation for the number of chains for cellulose nanocrystals (CNC)

Total number of chains in the CNC cross section

Considering that the average cross section of the CNC cylinder is 4 nm in diameter (r=2) and length of L:100 nm

Surface area of 1 CNC cylinder = 2πr2 + 2πrL =2.π.22 +  2.π.2.100  = 1282 nm2

Previously, Isogai [1] et al reported the two dimensions of anhydroglucose units (AGU) to be: a=0.61 nm and b= 0.54 nm - which are used to evaluate the surface area of a single AGU cell = a x b = 0.33 nm2

Thus, the number of AGU available on the surface of a single CNC is: 1282/0.33 = 3885 chains.

S2: SANS curve fitting procedure

The SANS scattering intensity, I(q), is related with the form factor (scattering amplitude) of long cylinder shell and distribution function as follows [2]:

Iq=0∞NrILongCylShellq2dr+Aq-α+Bkg

Where, N(r) is the lognormal distribution which is defined as:

Nr=1(2π)2 rσexp-ln(r/μ)2⁡2σ2

with, r > 0, µ is the mean and σ is the standard deviation of the CNC.

ILongCylShellq is the scattering amplitude (form factor) for a long cylinder shell defined as follows:-

ILongCylShellq=P'q Pcs(q)

Where,

P'q=    2 Si(qL)qL-( sin(qL/2)qL/2 )2

Six=0x Sin ttdt

Pcsq =   ( 2J1qRqR ηcore- ηshell R2 L π +2J1q(R+t)q(R+t) ηshell- ηsolv (R+t)2 L π )2

Where, R is the core radius, t is the shell thickness, L is the cylinder length, ηcore is the scattering length density of cylinder core, ηshell is the scattering length density of cylinder shell and ηsolv is the scattering length density of solvent. For the long cylinder the approximation is L >2r.

q is the magnitude of scattering vector which is related to the wavelength (λ) of the X-rays and the scattering angle (2θ) as follows:

q= 4πsinθλ

Further details on SAXS curve fitting and procedure are provided in the manual of SASfit [3].

Reference

[1] Yusuke Okita, Tsuguyuki Saito, and Akira Isogai, Entire Surface Oxidation of Various Cellulose Microfibrils by TEMPO-Mediated Oxidation, Biomacromolecules 2010, 11, 1696–1700.

[2] I. Breßler, J. Kohlbrecher and A. F. Thünemann, SASfit: a tool for small-angle scattering data analysis using a library of analytical expressions, J. Appl. Cryst. (2015). 48, 1587-1598,

[3] https://www.psi.ch/en/sinq/sansi/sasfit