# Supporting Information
Using neutron diffraction to explore lithium displacement within cubic phase stabilised Ga-doped Li6.75La3Zr1.75Ta0.25O12 lithium garnet oxides.

Timothy Daniel Christopher,1,2 Tianhang Zhang,3,4 Saifang Huang,3,5Zoran Zujovic,1,6 Maxim Avdeev,7,8 Peng Cao,2,3 Tilo Söhnel1,2,*

- School of Chemical Sciences and Centre for Green Chemical Science, University of Auckland, Private Bag 92019, Auckland 1142, New Zealand

- MacDiarmid Institute for Advanced Materials and Nanotechnology, Victoria University of Wellington, PO Box 600, Wellington 6140, New Zealand

- Department of Chemical and Materials Engineering, University of Auckland, Private Bag 92019, Auckland 1142, New Zealand

- School of Materials Science and Technology, Beijing Key Laboratory of Materials, Utilisation of Nonmetallic Minerals and Solid Wastes, National Laboratory of Mineral Materials, China University of Geosciences (Beijing), Beijing 100083, P. R. China

- School of Materials Science and Engineering, Jiangsu University of Science and Technology, Zhenjiang, 212003, P. R. China

- The NMR Centre, Faculty of Science, University of Auckland, Auckland, Private Bag 92019, Auckland 1010, New Zealand

- School of Chemistry, The University of Sydney, Sydney, New South Wales 2006, Australia

- Australian Nuclear Science and Technology Organisation, Lucas Heights, New South Wales 2234, Australia

*To whom correspondence should be addressed; e-mail:  t.soehnel@auckland.ac.nz.

Table S1. A summary of X-ray refinements for the Li6.45−3𝑥Ga𝑥La3Zr1.75Ta0.25O12 series from x = 0 to 0.5

| Gallium Content (x) | Phase(s) and Percentage | LGO Cubic Lattice Constant (Å) | Rp | Rwp |
| --- | --- | --- | --- | --- |
| 0 | LLZTO – Cubic : 58(2)%, LLZO – Tetragonal : 42(2) % | 12.93803(78) | 6.28 | 8.13 |
| 0.1 | Li6.45−3𝑥Ga𝑥La3Zr1.75Ta0.25O12 : 99.35(1.2)%, La2O3 : 0.65(15) % | 12.95044(17) | 6.80 | 8.63 |
| 0.2 | Li6.45−3𝑥Ga𝑥La3Zr1.75Ta0.25O12 : 99.4(1.2)%, La2O3 : 0.65(15) % | 12.95551(10) | 6.03 | 7.57 |
| 0.3 | Li6.45−3𝑥Ga𝑥La3Zr1.75Ta0.25O12 : 99.0(7) %, La2O3 :1.0(1) %) | 12.95516(12) | 6.63 | 5.6 |
| 0.4 | Li6.45−3𝑥Ga𝑥La3Zr1.75Ta0.25O12 :98.97(71) %, La2O3 : 1.15(68) % | 12.95940(11) | 6.27 | 7.94 |
| 0.5 | Li6.45−3𝑥Ga𝑥La3Zr1.75Ta0.25O12 : 96.8(7)%, La2O3: 0.75 (9)%, La2Zr2O7 : 2.42 (12) | 12.96059(13) | 6.66 | 8.42 |

Table S2. A summary of neutron refinements for the Li6.45−3𝑥Ga𝑥La3Zr1.75Ta0.25O12 series from x = 0 to 0.5

| Gallium Content (x) | Temperature (°C) | Cubic Lattice Constant (Å) | Rbragg | Rp | Rwp |
| --- | --- | --- | --- | --- | --- |
| 0.1 | 25 | 12.9556(2) | 3.75 | 2.76 | 3.57 |
| 0.1 | 200 | 13.0016(2) | 3.63 | 3.06 | 4.07 |
| 0.1 | 400 | 13.04238(24) | 4.50 | 3.16 | 4.27 |
| 0.1 | 600 | 13.08337(29) | 4.19 | 3.03 | 4.20 |
| 0.2 | 25 | 12.95980(14) | 3.37 | 2.61 | 3.30 |
| 0.2 | 200 | 13.00414(16) | 3.30 | 2.81 | 3.61 |
| 0.2 | 400 | 13.04361(19) | 3.86 | 2.81 | 3.65 |
| 0.2 | 600 | 13.08355(22) | 3.71 | 2.65 | 3.49 |
| 0.3 | 25 | 12.95829(21) | 4.87 | 2.86 | 3.66 |
| 0.3 | 200 | 13.00091(22) | 4.44 | 3.27 | 4.15 |
| 0.3 | 400 | 13.03919(25) | 4.86 | 3.46 | 4.55 |
| 0.3 | 600 | 13.07999(29) | 5.02 | 3.25 | 4.39 |
| 0.4 | 25 | 12.96144(16) | 3.69 | 2.88 | 3.53 |
| 0.4 | 200 | 12.99862(19) | 4.10 | 3.15 | 4.05 |
| 0.4 | 400 | 13.03688(22) | 4.64 | 3.05 | 4.05 |
| 0.4 | 600 | 13.07657(25) | 4.78 | 2.97 | 3.93 |
| 0.5 | 25 | 12.95442(19) | 4.17 | 3.79 | 5.15 |
| 0.5 | 200 | 12.99909(22) | 4.37 | 3.48 | 4.61 |
| 0.5 | 400 | 13.03849(26) | 4.84 | 3.36 | 4.62 |
| 0.5 | 600 | 13.07875(29) | 5.22 | 3.16 | 4.37 |

Figure S1. 7Li NMR spectrum of Li6.75-3xLa3Zr1.75Ta0.25O12 x = 0.5. The sidebands are denoted by asterisks.

7Li NMR spectrum is shown in Figure S1. The spectrum reveals a broad single peak at δ = 0.6 ppm flanked by the sidebands observed on either side, indicating the presence of 7Li within the lithium garnet system of Li6.75-3xLa3Zr1.75Ta0.25O12, x = 0.5.

Figure S2. (a) Average lanthanum to oxygen bond lengths (Å) and (b) LaO8 polyhedral volumes (Å3) versus temperature (°C) for Li6.75-3xGaxZr1.75Ta0.25O12. Datasets staggered for clarity.

Figure S3. (a) Average zirconium to oxygen bond lengths (Å) and (b) ZrO6 polyhedral volumes (Å3) versus temperature (°C) for Li6.75-3xGaxZr1.75Ta0.25O12. Zirconium represents the 7:1 ratio of zirconium to tantalum in the 16 a site. Datasets staggered for clarity.